Data Cards

| CARBON (C) (graphite) |  | SULFUR (S) |
| --- | --- | --- |
| Appearance: | Dull, black solid |  | Appearance: | Dull, yellow solid |
| Solubility in water: | Insoluble |  | Solubility in water: | Insoluble |
| Effect of heat: | Little change |  | Effect of heat: | Melts, burns with a blue flame |
| Electrical conductivity of solid: | Conducts |  | Electrical conductivity of solid: | Does not conduct |
| Electrical conductivity of solution: | Does not dissolve in water and so conductivity cannot be tested |  | Electrical conductivity of solution: | Does not dissolve in water and so conductivity cannot be tested |
| Reaction with dilute hydrochloric acid: | Does not react |  | Reaction with dilute hydrochloric acid: | Does not react |
| Reaction with dilute sulfuric acid: | Does not react |  | Reaction with dilute sulfuric acid: | Does not react |
| ZINC (Zn) |  | ALUMINIUM (Al) |
| Appearance: | Shiny, silver-grey solid |  | Appearance: | Shiny, silvery solid |
| Solubility in water: | Insoluble |  | Solubility in water: | Insoluble |
| Effect of heat: | No effect on moderate heating |  | Effect of heat: | No effect on moderate heating |
| Electrical conductivity of solid: | Conducts |  | Electrical conductivity of solid: | Conducts |
| Electrical conductivity of solution: | Does not dissolve in water and so conductivity cannot be tested |  | Electrical conductivity of solution: | Does not dissolve in water and so conductivity cannot be tested |
| Reaction with dilute hydrochloric acid: | Reacts to form a colourless solution; Gas produced |  | Reaction with dilute hydrochloric acid: | Does not react for a few minutes, then reacts to form a colourless solution; Gas produced |
| Reaction with dilute sulfuric acid: | Reacts to form a colourless solution; Gas produced |  | Reaction with dilute sulfuric acid: | Does not react |

Data cards

| COPPER (Cu) |  | COPPER OXIDE (CuO) |
| --- | --- | --- |
| Appearance: | Shiny, brown solid |  | Appearance: | Dull, black solid |
| Solubility in water: | Insoluble |  | Solubility in water: | Insoluble |
| Effect of heat: | Turns black |  | Effect of heat: | No effect |
| Electrical conductivity of solid: | Conducts |  | Electrical conductivity of solid: | Does not conduct |
| Electrical conductivity of solution: | Does not dissolve in water and so conductivity cannot be tested |  | Electrical conductivity of solution: | Does not dissolve in water and so conductivity cannot be tested |
| Reaction with dilute hydrochloric acid: | Does not react |  | Reaction with dilute hydrochloric acid: | Reacts ( when warmed) to form a blue solution |
| Reaction with dilute sulfuric acid: | Does not react |  | Reaction with dilute sulfuric acid: | Reacts to form a blue solution |
| COPPER CARBONATE (CuCO3) |  | CALCIUM CARBONATE (CaCO3) |
| Appearance: | Dull, green solid |  | Appearance: | Dull, white solid |
| Solubility in water: | Insoluble |  | Solubility in water: | Insoluble |
| Effect of heat: | Turns blacks - Gas produced |  | Effect of heat: | Little change |
| Electrical Conductivity of solid: | Does not conduct |  | Electrical Conductivity of solid: | Does not conduct |
| Electrical conductivity of solution: | Does not dissolve in water , so conductivity cannot be tested |  | Electrical conductivity of solution: | Does not dissolve in water , so conductivity cannot be tested |
| Reaction with dilute hydrochloric acid: | Reacts to form a blue solution; Gas produced |  | Reaction with dilute hydrochloric acid: | Reacts to form a colourless solution; Gas produced |
| Reaction with dilute sulfuric acid: | Reacts to form a blue solution; Gas produced |  | Reaction with dilute sulfuric acid: | Little effect |

| SODIUM CARBONATE (Na2CO3) |  | SODIUM CHLORIDE (NaCl) |
| --- | --- | --- |
| Appearance: | Dull, white solid |  | Appearance: | Dull, white solid |
| Solubility in water: | Soluble |  | Solubility in water: | Soluble |
| Effect of heat: | No effect |  | Effect of heat: | No effect |
| Electrical conductivity of solid: | Does not conduct |  | Electrical conductivity of solid: | Does not conduct |
| Electrical conductivity of solution: | Conducts; Gas produced |  | Electrical conductivity of solution: | Conducts; Gas produced : Chlorine smell |
| Reaction with dilute hydrochloric acid: | Reacts to form a colourless solution ; Gas produced |  | Reaction with dilute hydrochloric acid: | Dissolves to form a colourless solution |
| Reaction with dilute sulfuric acid: | Reacts to form a colourless solution; Gas produced |  | Reaction with dilute sulfuric acid: | Dissolves to form a colourless solution |
| MAGNESIUM OXIDE (MgO) |  | SUGAR (C11H22O11) |
| Appearance: | Dull, white solid |  | Appearance: | Dull, white solid |
| Solubility in water: | Insoluble |  | Solubility in water: | Soluble |
| Effect of heat: | No effect |  | Effect of heat: | Melts - Bubbles - Turns black |
| Electrical conductivity of solid: | Does not conduct |  | Electrical conductivity of solid: | Does not conduct |
| Electrical conductivity of solution: | Does not dissolve in water, so conductivity cannot be tested |  | Electrical conductivity of solution: | Does not conduct |
| Reaction with dilute hydrochloric acid: | Reacts to form a colourless solution |  | Reaction with dilute hydrochloric acid: | Dissolves to form a colourless solution |
| Reaction with dilute sulfuric acid: | Reacts to form a colourless solution |  | Reaction with dilute sulfuric acid: | Dissolves to form a colourless solution |

Data cards

Data cards

| COPPER SULFATE (CuSO4) |  |  |
| --- | --- | --- |
| Appearance: | Dull, blue solid |  |  |  |
| Solubility in water: | Soluble – forms blue solution |  |  |  |
| Effect of heat: | Forms white powder and water vapour |  |  |  |
| Electrical conductivity of solid: | Does not conduct |  |  |  |
| Electrical conductivity of solution: | Conducts; Copper deposited; Gas produced |  |  |  |
| Reaction with dilute hydrochloric acid: | Dissolves to form a blue solution |  |  |  |
| Reaction with dilute sulfuric acid: | Dissolves to form a blue solution |  |  |  |

# Text boxes

ACTIVITY 3.1:  TEN QUESTIONS

MP3.1F

MP3.1E

MP3.1D

MP3.1C

ACTIVITY 3.1:  TEN QUESTIONS

ACTIVITY 3.1:  TEN QUESTIONS

ACTIVITY 3.1:  TEN QUESTIONS